## Slide 1: Nanoparticle toxicity
Jérôme Neirynck, Frederik Van Eecke & Robin Vrielynck
prof. dr. Ewald Janssens & prof. dr. Kristiaan Temst
Advanced Topics in Clusters, Macromolecules & Nanoparticles (G0S94A)
Master of Physics
Faculty of Science – Department of Physics and Astronomy

## Slide 2: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 3: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 4: Nanoparticles in real life
Consumer products
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Nanoparticle-baised cometics
Nanocomposite parts
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001

## Slide 5: What is nanotoxicity?
= study of toxicity of nanomaterials
Inert materials become highly active at nanodimensions
Intended to determine whether or to what these properties pose a threat
Their most attractive properties make them also potentially toxic.
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001

## Slide 6: Properties of nanoscale materials
Their most attractive properties make them also potentially toxic.
Higher reactivity
Higher surface to mass ratio
Higher permeation
Properties of matter change at nanosize:
Colour
Chemical reactivity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001

## Slide 7: Silver nanoparticles
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Macro: anti-bacterial substance
Nano: detected in various organs of rats via inhalation
Toxicity depends on:
Cell viability
Reactive oxygen species
Dehydrogenase
Coating difference: peptide-coated VS citrate-coated
Dose
Conclusion: toxicity issue relate to experimental by using of standard protocols
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001
Notes: In vivo – in vitro – ex vivo

## Slide 8: Zinc oxide nanoparticles
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Applications: paint, UV detectors, gas sensors, sunscreens & personal care products
Studies have shown:
Cell death
Change cell morphology
DNA damage
Mitochondrial inactivity in kidney cells
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001
Notes: In vivo – in vitro – ex vivo

## Slide 9: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 10: Dose dependence
Not dependent on mass dose
Surface is reactive, so small particles at a low mass dose can be as toxic as larger particles with a higher mass dose
Surface dose is what influences the toxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 11: Size dependence
Even at the same surface dose size of particles has an effect
Smaller particles have
prolonged retention
higher translocation
higher effect on the functioning of the macrophages
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 12: Concentration dependence
Large concentration  aggregation of particles
Larger particles, less surface AND white bloodcells can macrophage the aggregates
Large concentration results in less toxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 13: Crystalline structure
Even for the same substance, a different crystalline structure may influence the toxicity
TiO2 has for instance two different structures, of which one is toxic, and the other one is nontoxic
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 14: Aspect ratio
Long fibers are more toxic than short ones
Stay longer in the body (81% after 60 days)
Can penetrate celmembrane
Carbon nanotubes can be toxic
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 15: Adaptation to nanoparticles
When first exposed to low doses of toxic nanoparticles for a period of time, there is not such a heavy reaction to a high dose
Habituation to the nanoparticles
White bloodcells fight more effectively against the nanoparticles
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.

## Slide 16: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 17: Exposure to nanoscale materials
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Inhalation
Oral ingestion
Skin contact
Source: Armstead, A. L., & Li, B. (2016). Nanotoxicity: emerging concerns regarding nanomaterial safety and occupational hard metal (WC-Co) nanoparticle exposure. International journal of nanomedicine, 11, 6421–6433. doi:10.2147/IJN.S121238

## Slide 18: Exposure to nanoscale materials
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Inhalation
Oral ingestion
Skin contact
EXTERNAL
INTERNAL
Direct exposure
Toxicity
Oxidative stress
DNA damage
Inflammation
PRIMARY EFFECTS
Tissue & organ deposition
Systematic inflammation
Altered functionality
SECONDARY EFFECTS
Source: Armstead, A. L., & Li, B. (2016). Nanotoxicity: emerging concerns regarding nanomaterial safety and occupational hard metal (WC-Co) nanoparticle exposure. International journal of nanomedicine, 11, 6421–6433. doi:10.2147/IJN.S121238

## Slide 19: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 20: Tests for toxicity
Measurement parameters:
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
duration & route
of exposure
dosage & composition
of test material
reference material need to be provided to compare
what biological environment is used?
Response of biological environment to the nanoparticles can extremely vary!
Source: Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001

## Slide 21: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 22: Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:
Characterization
In Vitro Toxicity
In Vivo Toxicity
Predictive Modeling

## Slide 23: Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:
Area 1: Nanoparticle characterization
Nanoparticles are first assessed in the as-synthesized form after dispersion in the appropriate aqueous media.
Determination of:
Concentration
Composition
Size
Surface area
Morphology
charge

## Slide 24: Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:
Area 2: In Vitro toxicity
Study influence on subcellular, cellular and whole tissue.
Determination of:
A relatively simple model that reveals a general mechanism of toxicity can be a basis for further assessment.
“elementary toxicity”: the ability of a compound to cause death as a consequence of damage to basic cellular functions.
Experimental observation:
“The data obtained from basal toxicity studies have been found to be in good correlation with acute toxicity in animals and humans”

## Slide 25: Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:
Area 3: In Vivo
= Test results from In Vitro experiments
Test for effects on:
  immune system response
  Translocation to other areas after uptake
Area 4: Toxicokinetic modeling
describes the absorption, distribution, metabolism and elimination of xenobiotics (foreign materials) within an organism, as a function of dose and time.

## Slide 26: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 27: Genotoxicity
Study of physical and chemical agents that can damage the genetic materials of cells
DNA damage, which can lead to cancer
Inherting changes in DNA from one generation to next
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Phillips D.H., Arlt V.M. (2009) Genotoxicity: damage to DNA and its consequences. In: Luch A. (eds) Molecular, Clinical and Environmental Toxicology. Experientia Supplementum, vol 99. Birkhäuser Basel
Notes: In vivo – in vitro – ex vivo

## Slide 28: DNA mutations
Ideal: DNA sequence do not change, except during reproduction
Reality: DNA damage due to cell process & toxic chemicals
robust repair mechanism
DNA is repaired incorrectly
mutations
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
no or minor effect
life-threatening effects
when occured in wrong place
Source: Phillips D.H., Arlt V.M. (2009) Genotoxicity: damage to DNA and its consequences. In: Luch A. (eds) Molecular, Clinical and Environmental Toxicology. Experientia Supplementum, vol 99. Birkhäuser Basel
Notes: In vivo – in vitro – ex vivo

## Slide 29: DNA mutations
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Compounds do not correspond (4)
Structure of DNA string is broken (2)
Source: Phillips D.H., Arlt V.M. (2009) Genotoxicity: damage to DNA and its consequences. In: Luch A. (eds) Molecular, Clinical and Environmental Toxicology. Experientia Supplementum, vol 99. Birkhäuser Basel
Notes: In vivo – in vitro – ex vivo

## Slide 30: DNA mutations
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Origin of DNA damage:
Ionizing radiation
Chemicals
Formation of reactive oxygen species
Source: Phillips D.H., Arlt V.M. (2009) Genotoxicity: damage to DNA and its consequences. In: Luch A. (eds) Molecular, Clinical and Environmental Toxicology. Experientia Supplementum, vol 99. Birkhäuser Basel
Notes: In vivo – in vitro – ex vivo

## Slide 31: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 32: Contradicting results for CNT toxicity
Lam et al., 2004
Dose dependent lesions: inflammation, fibrosis and necrosis
Foreign-body reactions
More lymphocytes
Warheit et al., 2004
Non-dose dependent lesions
No prolonged inflamation in the lungs
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 33: Reason for differences
Different way of preparing samples  different diffusion in the lungs
Different fabrication method of CNTs gives different "purity"
In the Warheit et al. experiment lots of the bolus didn't reach the alveolar region
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 34: CNT toxicity
Overview
Impurities
Long fiber macro phagocytosis
Oxidative potential
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 35: Impurities
Encased in carbon shell  no interaction with cells
During ultrasonication (toxic) impurities can be released
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 36: Long fibers
CNTs bundel into ropes due to van der Waals forces
Makes long asbestos fibers
Penetrate cell membrane
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 37: Oxidative stress
CNTs can be good conductors
Shifting electrons between cells
Oxidation and reduction
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source: Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.

## Slide 38: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 39: In silico models to predict BBB permeation of nanoparticles
The mechanism for different NP’s at the BBB is a fundamental parameter to asses and predict their nanotoxic potential for the CNS.
Why in silico models, support in:
  Data mining of large databases.
  Network analysis.
  Molecular dynamics (MD) simulations for the so-called ADMET.
  Regulatory demand for advancing the use of alternative non-animal testsystems.
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 40: Main issue: Permeation of NP through a lipid membrane
Difficulties:
Permeation mechanism is complex and depending on :
  Size
  Aggregation state
  Surface charge
  Zeta (f) potential
Size of computations (Atoms and time)
Solve:
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 41: Coarse-grained MD models
Model for simplified representation.
using ‘‘pseudoatoms” for the representations of the NP and membrane geometries
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 42: Results from model using dissipative particles
Some very small or very hydrophobic NPs may just pass the BBB.
Hydrophobic NP insert lipid bilayer spontaneously
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 43: Future opportunities
“A more intensive effort towards the development of predictive toxicity models is urgently needed.”
Problems:
The development of predictive models, particularly computational models, requires large amounts of high quality data
do not include a detailed description of the tested materials, measure different endpoints
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 44: The road to succes
There must be greater standardization at all stages of the toxicity studies, data collected in the same manner are needed.
studies should be designed in ways that specifically and systematically evaluate the role of physico-chemical properties in MNM behavior.
Systematic testing of variations on a NP property (e.g., charge, size, surface properties, etc.) are needed to identify how physicochemical properties influence biological activity.
an open system for storing and sharing information is needed.
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
Source:

## Slide 45: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 46: Nanofood
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
PACKING
Active packing
constantly provides certain feature
e.g. stop oxygen from spoiling food
antimicrobial films in beer bottles
Smart packing
reacts to changes in environment
e.g. presence of pathogens that can produce diseases
Source: AZoNano. (2006). Nanofood Defined and The Use Of Nanotechnology In Packaging, Producing and Growing Foods Now and Into The Future, https://www.azonano.com/article.aspx?ArticleID=1786
Future of packing
reflecting heat ox ice cream boxes
self healing packing
milk carton that changes colour

## Slide 47: Nanofood
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
FOOD PROCESSING
Nanoparticles & nanocapsules
change taste, alter properties
e.g. tuna oil (omega 3) in bread
avoid unpleasant taste
FARMING
Nanosensors
nutrient levels, water concentration, pests,…
Nanochips
tracking, information about vaccines
AGRICULTURE
ANIMALS
Source: AZoNano. (2006). Nanofood Defined and The Use Of Nanotechnology In Packaging, Producing and Growing Foods Now and Into The Future, https://www.azonano.com/article.aspx?ArticleID=1786

## Slide 48: Outline
Introduction: What is toxicity?
Parameters influencing toxicity
Exposure of nanoparticles
Testing nanotoxicity
Areas studied for nanotoxicity
J. Neirynck, F. Van Eecke & R. Vrielynck
Application: Genotoxicity
Application: CNT toxicity
Modelling of nanotoxity
Nanofood
Conclusion

## Slide 49: Conclusion
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
NANOTECHNOLOGY
BENEFITS & APPLICATIONS
NANOTOXICITY
Diseases
Genotoxicity
CNT toxicity
Important tools at molecular level
Source: Buzea, C., Pacheco, I.I. & Robbie, K. Biointerphases (2007) 2: MR17. https://doi.org/10.1116/1.2815690

## Slide 50: Conclusion
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary
RESEARCH ON NANOTOXICITY
Relation nanoparticle properties & toxicity
Kinetics & biochemical interactions within orgaisms
emperical evaluation
Nanoparticle aging
Surface modifications
Environment effects
Translocation pathways
Short- & long-term toxicity
Interaction effect on toxicity?
MULTIDISCIPLINARY APPROACH
Source: Buzea, C., Pacheco, I.I. & Robbie, K. Biointerphases (2007) 2: MR17. https://doi.org/10.1116/1.2815690

## Slide 51: References
Bahadar, H., Maqbool, F., Niaz, K., & Abdollahi, M. (2016). Toxicity of Nanoparticles and an Overview of Current Experimental Models. Iranian biomedical journal, 20(1), 1–11. doi:10.7508/ibj.2016.01.001
Buzea, Cristina, Ivan I. Pacheco, and Kevin Robbie. "Nanomaterials and nanoparticles: sources and toxicity." Biointerphases 2.4 (2007): MR17-MR71.
Armstead, A. L., & Li, B. (2016). Nanotoxicity: emerging concerns regarding nanomaterial safety and occupational hard metal (WC-Co) nanoparticle exposure. International journal of nanomedicine, 11, 6421–6433. doi:10.2147/IJN.S121238
Phillips D.H., Arlt V.M. (2009) Genotoxicity: damage to DNA and its consequences. In: Luch A. (eds) Molecular, Clinical and Environmental Toxicology. Experientia Supplementum, vol 99. Birkhäuser Basel
Lam, Chiu-wing, et al. "A review of carbon nanotube toxicity and assessment of potential occupational and environmental health risks." Critical reviews in toxicology 36.3 (2006): 189-217.
Buzea, C., Pacheco, I.I. & Robbie, K. Biointerphases (2007) 2: MR17. https://doi.org/10.1116/1.2815690
AZoNano. (2006). Nanofood Defined and The Use Of Nanotechnology In Packaging, Producing and Growing Foods Now and Into The Future, https://www.azonano.com/article.aspx?ArticleID=1786
J. Neirynck, F. Van Eecke & R. Vrielynck
Introduction Framework Techniques & Results Summary